## Slide 1: HYPERION– The Venice pilot case
1

## Slide 2
Classification of the building materials and characterisation of their petrographic, petrophysical and mechanical properties;
Characterization and mapping of the decay forms and products;
Installation of a network of sensors to provide micro-climate data to an Hygro-Thermal Simulator tool used to model the hygrothermal behaviour of the material exposed to different micro-climate conditions;
Design and installation of a novel experimental setup to determine stone deterioration under outdoor conditions, monitoring surface temperature and moisture on slabs exposed at different orientations (north, south, and horizontal plane);
Evaluation of the recession rate of the carbonate stones in laboratory experiments under different rainwater compositions and accounting for their textural features (e.g. calcite grain-size)
Investigations performed at the pilot site of Venice

## Slide 3: Classification and mapping of materials at Tier 1 building Clock Tower
2 mm
Istria stone
2 mm
Red Verona Stone
2 mm
Carrara marble
2 mm
Prun Stone
2 mm
Proconnesian marble
Main rock types
Decay products analyses
Mapping

## Slide 4
Detachment
  Material
  Loss
  Biological
  Colonization
  Cracks
  &
  Deformation
  Discoloration
  &
  Deposit
  Method from ICOMOS-ISCS Illustrated glossary on stone deterioration patterns (2008) combined with Fitzner & Heinrichs (2001)
Main results:
Lithological mapping
Maps of decay
Petrographic analysis
Physical features (porosity)
Study of deterioration patinas
Mapping of deterioration pattern at Tier 1 building Clock Tower

## Slide 5
Hyperspectral survey on the Clock Tower façade
Mapping of deterioration pattern at Tier 1 building Clock Tower

## Slide 6
Control unit box and main component boards
Experimental installation at Venice
Main results:
Cubes installation
Smart tags installation
Weathering station installation
Test monitoring of surface temperature
Air temperature and RH in the Tier 1 Clock Tower
The Smart Tag and the weather station provided by the Hyperion partners.
Experimental setup to determine stone deterioration at different orientations

## Slide 7
Correlation between average grain size and average recession measured on 11 carbonate rocks after 240 aging cycles.
3D surface models for limestones before aging (left) and after (right) 240 aging cycles. On the top: Chiampo paglierino sample. On the bottom: Botticicino limestone.
Evaluation of the recession rate under different rainwater compositions and grain size

## Slide 8: Thank you all!
Claudio Mazzoli, UNIPD: | claudio.mazzoli@unipd.it